Surface-PASylation of ferritin to form stealth nanovehicles enhances in vivo therapeutic performance of encapsulated ellipticine

Barbora Tesarovaa,b,1, Simona Dostalovaa,b, Veronika Smidovaa,b, Zita Goliasovaa,b, Zuzana Skubalovaa,b, Hana Michalkovaa,b, David Hyneka,b, Petr Michaleka,b, Hana Polanskac, Marketa Vaculovicovaa,b, Jaromir Hacekd, Tomas Eckschlagere, Marie Stiborovaf, Ana S. Piresg,h, Ana R.M. Nevesh, Ana M. Abrantesg,h, Tiago Rodrigues i, Paulo Matafomei, Maria F. Botelhog,h, Paulo Teixeirag,j,k, Fernando Mendesg,h,k, Zbynek Hegera,b,∗

a Department of Chemistry and Biochemistry, Mendel University in Brno, Zemedelska 1, CZ, 613 00, Brno, Czech Republic b Central European Institute of Technology, Brno University of Technology, Purkynova 656/123, CZ, 612 00, Brno, Czech Republic c Department of Pathological Physiology and Department of Physiology, Faculty of Medicine, Masaryk University, Kamenice 753/5, CZ,625 00, Brno, Czech Republic d Department of Pathology and Molecular Medicine, Second Faculty of Medicine, Charles University and University Hospital Motol, V Uvalu 84, CZ, 150 06, Prague 5, Czech Republic e Department of Paediatric Haematology and Oncology, Charles University and University Hospital Motol, V Uvalu 84/1, CZ, 150 06, Prague 5, Czech Republic f Department of Biochemistry, Faculty of Science, Charles University, Hlavova 2030/8, CZ,128 43, Prague 2, Czech Republic g CNC.IBILI Consortium/Centre for Innovative Biomedicine and Biotechnology (CIBB), University of Coimbra, Azinhaga de Santa Comba, Celas, 3000-548, Coimbra, Portugal h Biophysics Institute, Coimbra Institute for Clinical and Biomedical Research (iCBR) area of Environment Genetics and Oncobiology (CIMAGO), Faculty of Medicine, University of

Coimbra, Azinhaga de Santa Comba, Celas, 3000-548 Coimbra, Portugal i Institute of Physiology and Coimbra Institute for Clinical and Biomedical Research (iCBR), CNC.IBILI - Faculty of Medicine, University of Coimbra, Azinhaga de Santa Comba, Celas,

3000-548, Coimbra, Portugal j Pathology Department, Coimbra Hospital and Universitary Centre, Praceta Prof. Mota Pinto, 3000-075 Coimbra, Portugal k Polytechnic Institute of Coimbra, ESTESC-Coimbra Health School, Department Biomedical Laboratory Sciences, Rua 5 de Outubro, 3046-854, Coimbra, Portugal

a b s t r a c t

Surface functionalisations substantially influence the performance of drug delivery vehicles by improv- ing their biocompatibility, selectivity and circulation in bloodstream. Herein, we present the study of in vitro and in vivo behaviour of a highly potent cytostatic alkaloid ellipticine (Elli) encapsulated in internal cavity of ferritin (FRT)-based nanocarrier (hereinafter referred to as FRTElli). In addition, FRTElli sur- face was functionalised with three different molecular coatings: two types of protective PAS peptides (10- or 20-residues lengths) with sequences comprising amino acids proline (P), alanine (A) and ser- ine (S) (to form PAS-10-FRTElli or PAS-20-FRTElli, respectively), or polyethylene glycol (PEG-FRTElli). All three surface modifications of FRT disposed sufficient encapsulation efficiency of Elli with no premature cumulative release of cargo. Noteworthy, all tested surface modifications displayed beneficial effects on the in vitro biocompatibility. PAS-10-FRTElli exhibited markedly reduced uptake by macrophages com- pared to PAS-20-FRTElli, PEG-FRTElli or unmodified FRTElli. The exceptional properties of PAS-10-FRTElli were validated by an array of in vitro analyses including formation of protein corona, uptake efficiency or screenings of selectivity of cytotoxicity. In murine preclinical model bearing triple-negative breast cancer (MDA-MB-231) xenograft, compared to free Elli or FRTElli, PAS-10-FRTElli displayed enhanced accumu- lation of Elli within tumour tissue, while hampering the uptake of Elli into off-target tissues. Noteworthy, PAS-10-FRTElli led to decreased in vivo complement (C3) activation and protein corona formation. Taken together, presented in vivo results indicate that PAS-10-FRTElli represents a promising stealth platform for translation into clinical settings.